E-Mail : director@petroleumbazaar.com

113, Sona Shopping Centre, Cinestar Compound, Trikamdas Road, Kandivali (West) Mumbai – 400067     022-28077450, 28017099 Fax : 28017099

Ref. PBL.Spec.20

# SPECIFICATIONS

### “Bio Diesel”

| Component | ## Bio Diesel | ## EN 14214 ## Specification |
| --- | --- | --- |
| Ester Content | 97.3 % | 96.5 % min |
| Density | 870 | 860- 890 kg/m3 |
| Viscosity | 3.7 cSt | 3.5 to 5.0 cSt. |
| Flash Point | ~ 1500 C | 1200 C Min |
| Sulphur Content | Nil | 10 ppm Max. |
| Carbon Residue | 0.21% | 0.3% Max. |
| Cetane Number | 65.8 | 51.0 Min. |
| Sulphated Ash | 0.012% | 0.02% Max. |
| Water Content | 300 ppm | 500 ppm Max. |
| Cu Strip Corrosion | ~ class 2 | Class 1 |
| Oxidation Stability | ~6.7 | 6 h Min. |
| Acid Value | 0.5 | 0.5 mg/KOH |
| Iodine Value | 56 | 120 Max. |
| Poly unsaturated methyl ester | 0 | 1%Max. |
| Methanol | 0.005 % | 0.2% Max. |
| Monoglyceride | 0.7 % | 0.8% Max. |
| Diglyceride | 0.15 % | 0.2% Max. |
| Triglyceride | 0.1 % | 0.2% Max |
| Free Glycerol | 0.01 % | 0.02% Max. |
| Total Glycerol | 0.22 % | 0.25% |
| Group I metals (Na +K) | 4 ppm | 5 ppm Max.. |
| Group II Metals (Ca + Mg) | 0 ppm | 5 ppm Max.. |
| Phosphorus Content | 0 | 10 ppm Max. |
| Pour Point | 150 C | Not Specified |
| Colour (1” cell) | 28 units | Not Specified |

- The photo copies of following licences are required - Sales Tax / Vat licence, C form in case of out of state transportation,

- The price is subject to change. Pl confirm before placing order.

- Payment in Advance in favour of Petroleum Bazaar.com India Pvt Ltd. payable at Mumbai

- Specification as provided by the manufacturer

- For sample, price, delivery and availability pl contact Anupama / Vishakha at 022 28077450, 28017099